- INTERNATIONAL ELECTROTECHNICAL COMMISSION (IEC) SYSTEM FOR CERTIFICATION TO STANDARDS RELATING TO EQUIPMENT FOR USE IN EXPLOSIVE ATMOSPHERES (IECEx SYSTEM)

- Title:  ExTAG/602B/CD - Draft ExTAG Decision Sheet - Materials used to maintain a Sealed Device

- Circulated to: ExTAG – IECEx Testing and Assessment Group

INTRODUCTION

This document, ExTAG/602B/CD Draft ExTAG Decision Sheet - Materials used to maintain a Sealed Device, has been prepared by UL, LLC, US, incorporating comments provided on version ExTAG/602A/CD and is listed for discussion during the 2020 ExTAG Remote Meeting.

Changes to the original version are shown via tracking.

A Compilation of Comments on ExTAG/602A/CD, along with originator observations, are contained in ExTAG/618A/CC.

Christine Kane

ExTAG Secretariat

Address: IECEx Secretariat Level 33 Australia Square 264 George Street Sydney NSW 2000 Australia Web: www.iecex.com

- COLLECTION OF IECEx / ExTAG DECISION

| Standard: IEC 60079-15:2017 (Edition 5.0) | Clause: 9.1 |  |
| --- | --- | --- |
| Subject: Materials used to maintain a Sealed Device Status of document: Draft | Key words: - Sealed Device - Sealed Device materials - Seal material - Production control | - Date: 2020 07 20 Originator of original proposals: UL Originator of this text UL TC/SC involved: MT 60079-15 |
| Background: There have been inconsistencies between certification bodies regarding the application of construction requirements and the related production control for Sealed Devices. Portions of the first and second paragraphs from clause 9.1 of IEC 60079-15:2017 are provided below: “…Where the device is constructed with a separate housing and base that are sealed together, the housing and base of the device are not considered to be part of the seal.” “The documents according to IEC 60079-0 shall include a datasheet or statement from the sealed device manufacturer to show that the materials used for the seals have a thermal stability adequate for the service temperature range to which they will be subjected. The materials used for the seals shall have a continuous operating temperature (COT) range that includes a minimum temperature that is below, or equal to, the minimum service temperature and a maximum temperature that is at least 10 K above the maximum service temperature. This data sheet or statement may be on the sealing or encapsulating material, or may be on the overall sealed device itself.” The definition of a Sealed Device in clause 3.1.3 of IEC 60079-15:2017 states that the device is “….sealed effectively to prevent entry of an external atmosphere.” The definition implies that all materials and construction features preventing the entry of the external atmosphere into the sealed device are critical to maintain the method of protection. Misunderstanding of Clause 9.1 of IEC 60079-15:2017 could lead to a conclusion that production control is not necessary for all of the materials used to prevent entry of the external atmosphere into the internal compartment of the Sealed Device. Question: Are all parts of the Sealed Device relevant to maintaining the type of protection by preventing entry of the external atmosphere into the Sealed Device to be identified in the technical documentation? Answer: All parts which prevent the entry of the external atmosphere into the sealed device shall be identified in the technical documentation as they are relevant to maintaining the type of protection. Control of production of Ex equipment is governed by ISO/IEC 60079-34, the equipment manufacturer is responsible to control all critical parts and assembly of the equipment. Further, it must be understood that simply referencing a national, regional or international general industrial certification of a sealed device does not provide the production control necessary for Ex applications, as such general industrial certifications often include the use of multiple alternate materials. Refer also to clause 4.1.5 of OD017 for additional guidance. |  |  |